Construction Specification 762—Grouted Rock Riprap

1.	Scope

The work consists of furnishing, transporting, and the installation of concrete grout in the construction of grouted rock riprap revetments shown on the drawings.

2.	Material

Aggregates shall conform to the requirements of Section 801, Coarse Aggregates, and Section 802, Fine Aggregates, of the latest edition of the Alabama Department of Transportation Standard Specifications for Highway Construction.

Portland cement shall conform to the requirements of Section 815, Cement, of the latest edition of the Alabama Department of Transportation Standard Specifications for Highway Construction.

Fly ash shall conform to the requirements of Section 806, Mineral Admixtures, of the latest edition of the Alabama Department of Transportation Standard Specifications for Highway Construction.

Air-entraining admixtures shall conform to the requirements of Section 808, Air Entraining Additives, of the latest edition of the Alabama Department of Transportation Standard Specifications for Highway Construction. If air-entraining cement is used, any additional air-entraining admixture shall be of the same type as that in the cement.

Water reducing and/or retarding admixtures shall conform to the requirements of Section 809, Chemical Admixtures for Concrete, of the latest edition of the Alabama Department of Transportation Standard Specifications for Highway Construction.

Curing compound shall conform to the requirements of Section 830, Concrete Curing Materials, of the latest edition of the Alabama Department of Transportation Standard Specifications for Highway Construction.

Water used in mixing and curing concrete shall be clean and free from injurious amounts of oil, salt, acid, alkali, organic matter, or other deleterious substances.  Water shall conform to the requirements of Section 807, Water, of the latest edition of the Alabama Department of Transportation Standard Specifications for Highway Construction.

3.	Design of the grout mix

The mix proportions for the grout mix shall be as specified in the construction details in section 10 of this specification. During installation, the engineer may require adjustment of the mix proportions whenever necessary. The mix shall not be altered without the approval of the engineer.

4.	Handling and measurement of grout material

Material shall be stockpiled and batched by methods that prevent segregation or contamination of aggregates and ensure accurate proportioning of the mix ingredients.

Except as otherwise provided in section 10 of this specification, cement and aggregates shall be measured as follows:

•	Cement shall be measured by weight or in bags of 94 pounds each. When cement is measured in bags, no fraction of a bag shall be used unless weighed.

•	Aggregates shall be measured by weight. Mix proportions shall be based on the batch weight of each aggregate saturated, surface-dry weight plus the weight of surface moisture it contains at the time of batching.

•	Water shall be measured, by volume or by weight, to an accuracy within 1 percent of the total quantity of water required for the batch.

•	Admixtures shall be measured within a limit of accuracy of plus or minus 3 percent.

5.	Mixers and mixing

The mixer, when operating at capacity, shall be capable of combining the ingredients of the grout mix into a thoroughly mixed and uniform mass and of discharging the mix with a satisfactory degree of uniformity.

The mixer shall be operated within the limits of the manufacturer's guaranteed capacity and speed of rotation.

The time of mixing after all cement and aggregates have been combined in the mixer shall be a minimum of 1 minute for mixers having a capacity of 1 cubic yard or less. For larger capacity mixers, the minimum time shall be increased 15 seconds for each cubic yard or fraction thereof of additional capacity. The batch shall be so charged into the mixer that some water will enter in advance of the cement and aggregates, with the balance of the mixing water introduced into the mixer before a fourth of the total minimum mixing time has elapsed.

When ready-mix grout is furnished, the contractor shall furnish to the engineer at the time of delivery a ticket showing the time of loading and the quantities of material used for each load of grout mix delivered.

No mixing water in excess of the amount required by the approved job mix shall be added to the grout mix during mixing or hauling or after arrival at the delivery point.

6.	Conveying and placing

The grout mix shall be delivered to the site and placed within 1.5 hours after the introduction of the cement to the aggregates. In hot weather or under conditions contributing to accelerated stiffening of the concrete, the time between the introduction of the cement to the aggregates and complete discharge of the grout batch shall be a maximum of 45 minutes. The engineer may allow a longer time provided the setting time of the grout is increased a corresponding amount by the addition of an approved set-retarding admixture. In any case concrete shall be conveyed from the mixer to the final placement as rapidly as practicable by methods that prevent segregation of the aggregates, loss of mortar, displacement of the rock riprap, or a combination of these.

Grout mix shall not be allowed to free fall more than 5 feet unless suitable equipment is used to prevent segregation.

The grout mix shall not be placed until the rock riprap has been inspected and approved by the engineer for the placement of grout.

Rock to be grouted shall be kept moist for a minimum of 2 hours before grouting.

The rock riprap shall be flushed with water before placing the grout to remove the fines from the rock surfaces. The rock shall be kept moist before the grouting and without placing in standing or flowing water. Grout placed on inverts or other nearly level areas may be placed in one operation. On slopes, the grout shall be placed in two nearly equal applications consisting of successive lateral strips about 10 feet in width starting at the toe of the slope and progressing upward. The grout shall be delivered to the place of final deposit by approved methods and discharged directly on the surface of the rock. A metal or wood splash plate is used to prevent displacement of the rock directly under the grout discharge. The flow of grout shall be directed with brooms, spades, or baffles to prevent grout from flowing excessively along the same path and to assure that all intermittent spaces are filled. Sufficient barring shall be conducted to loosen tight pockets of rock and otherwise aid in the penetration of grout to ensure the grout fully penetrates the total thickness of the rock blanket. All brooming on slopes shall be uphill. After the grout has stiffened, the entire surface shall be rebroomed to eliminate runs and to fill voids caused by sloughing. The surface finish, following the completion of grout installation, shall consist of one-third of the rock extended above the level of grout. The exposed rock will not have a plastered appearance.

After completion of any strip or panel, no individual(s) or equipment shall be permitted on the grouted surface for 24 hours. The grouted surface shall be protected from injurious action by the sun, rain, flowing water, mechanical injury, or other potential damaging activity.

7.	Curing and protection

The completed finished surface shall be prevented from drying for a minimum curing period of 7 days following placement. Exposed surfaces shall be maintained in a moist condition continuously for the 7-day curing period or until curing compound has been applied as specified in this section. Moisture shall be maintained by sprinkling, flooding, or fog spraying or by covering with continuously moistened canvas, cloth mats, straw, sand, or other approved material. Water or moist covering shall be used to protect the grout during the curing process without causing damage to the grout surface by erosion or other mechanisms that may cause physical damage.

The grouted rock may be coated with an approved curing compound as an alternative method to maintaining a continuous moisture condition during the curing period. The compound shall be sprayed on the moist grout surface as soon as free water has disappeared and all surface finishing has been completed. The compound shall be applied at a minimum uniform rate of 1 gallon per 175 square feet of surface and shall form a continuous adherent membrane over the entire surface. Curing compound shall not be applied to surfaces requiring bond to subsequently placed grout and/or concrete. If the membrane is damaged during the curing period, the damaged area shall be resprayed at the rate of application specified for the original treatment.

Grout mix shall not be placed when the daily minimum temperature is less than 40 degrees Fahrenheit unless facilities are provided to ensure that the temperature of the material is maintained at a minimum temperature of 50 degrees Fahrenheit and not more than 90 degrees Fahrenheit during placement and the curing period. Grout mix shall not be placed on a frozen surface. When freezing conditions prevail, rock to be grouted must be covered and heated to within a range of 50 to 90 degrees Fahrenheit for a minimum of 24 hours before placing grouting material.

8.	Inspecting and testing fresh grout

The grout material shall be checked and tested throughout the grouting operation. Sampling of fresh grout shall be conducted in conformance with ASTM C 172. The volume of each batch will be determined by methods prescribed in ASTM C 138.

The engineer shall have free access to all parts of the contractor's plant and equipment used for mixing and placing grout during the period of the contract. Proper facilities shall be provided for the engineer to sample material and view processes implemented in the mixing and placing of grout as well as for securing grout test samples. All tests and inspections shall be conducted so that only a minimum of interference to the contractor's operation occurs.

For ready-mixed grout, the contractor shall furnish to the engineer a statement-of-delivery ticket for each batch delivered to the site. The ticket shall provide as a minimum: weight in pounds of cement, aggregates (fine and coarse), water; weight in ounces of air-entraining agent; time of loading; and the revolution counter reading at the time batching was started.

9.	Measurement and payment

Method 1—For items of work for which specific unit prices are established in the contract, the volume of grouted rock riprap, including filter layers or bedding, is determined to the nearest cubic yard from the specified thickness shown on the drawings and the area on which acceptable placement has been installed. Payment for grouted rock riprap is made at the contract unit price. Such payment is considered full compensation for all labor, material, equipment, and all other items necessary and incidental to the completion of the grouted rock riprap, filter layers and bedding, and geotextile material.

Method 2—For items of work for which specific unit prices are established in the contract, the volume of riprap and the volume of filter layers or bedding is determined to the nearest cubic yard from the specified thickness shown on the drawings and the area in which acceptable placement has been installed. The volume of grout is determined from the calculated batch volume and the number of mixed batches delivered to the site and placed in accordance with the specification. The area of geotextile is determined to the nearest square yard from measurements of geotextile material installed according to the contract requirements. Payment is made at the contract unit price for each type of rock riprap, filter or bedding, concrete grout, and geotextile. Such payment is considered full compensation for all labor, material, equipment, and all other items necessary and incidental to the completion of the work.

Method 3—For items of work for which specific unit prices are established in the contract, the quantity of each type of rock riprap placed within the specified limits is computed to the nearest 0.1 ton by actual weight. The quantity of each type of filter or bedding aggregate delivered and placed within the specified limits is computed to the nearest 0.1 ton. For each load of rock riprap placed as specified, the contractor shall furnish to the engineer a statement-of-delivery ticket showing the weight to the nearest 0.1 ton. For each load of filter or bedding aggregate, the contractor shall furnish to the engineer a statement-of-delivery ticket showing the weight to the nearest 0.1 ton. The volume of grout is determined from the calculated batch volume and the number of mixed batches delivered to the site and placed in accordance with the specifications and drawings. The area of geotextile is determined to the nearest square yard from measurements of geotextile material installed according to the contract requirements. Payment is made at the contract unit price for each type of rock riprap, filter or bedding, concrete grout, and geotextile. Such payment is considered full compensation for all labor, material, equipment, and all other items necessary and incidental to the completion of the work.

All methods—The following provision applies to all methods of measurement and payment. Compensation for any item of work described in the contract, but not listed in the bid schedule is included in the payment for the item of work to which it is made subsidiary. Such items and the items to which they are made subsidiary are identified in section 10 of this specification.

10.	Items of work and construction details

Items of work to be performed in conformance with this specification and the construction details therefore are:

Bid Item 19, Concrete Grout

- This item shall consist of furnishing and placing concrete grout on those portions of the riprap as shown on the drawings.

- The grouting mixture shall be as follows:

  - Cement: Type IA, Type I or Type II with an air entraining admixture, 6 sacks or 564 lbs/c.y.

  - Fine Concrete Aggregate: 1,128 lbs./c.y. (surface dry weight)

  - Coarse Concrete Aggregate: Pea Gravel, 1,692 lbs/c.y. (surface dry weight). Size No. 67, 7 or 8 as per ASTM C-33.

  - Water: 45 gal./c.y., or enough to provide a thick creamy consistency.

  - Air Content: 6 to 10 percent.

- Other similar grout mixes that incorporate small coarse aggregate may be used but must be approved by the Engineer.

- The grout shall be consolidated into the voids with the use of a concrete vibrator.

- Grouting operation shall not be performed except in the presence of the Engineer.

- A smooth surface is not to be created by the grouting operation.

- The average rate of grout application shall be 1.5 cubic feet of grout per square yard of loose rock riprap.  Permit the tops of some rock to stick up 1 to 3 inches above the neat lines shown on the drawings to ensure a rough surface.

- Curing compound shall be applied to the grout surface as soon as free water has disappeared from the surface of the grout, but shall no be applied to any surface until finishing of the surface is completed.

- Flowing water shall not be allowed in contact with the grout for a minimum of 24 hours as approved by the Engineer.

- Measurement and payment shall be by Method